## Slide 1: Current Project and New Idea Review
2026-10-22
Corrosion Technical Committee Name
Committee Chair: Mohsen Achour, ConocoPhilips
PRCI Support Staff: Janie Norton

## Slide 2: TC Research Area Name: CORR – Crack Management (Part of SRP) Idea/Project Name: EC-08-13 Influence of External Hydrogen on Crack Growth Research Objective Alignment: Confirm the fundamental integrity and safe operation of vintage pipelines
Idea/Project Overview
Brief description of technology: Project aims to address knowledge gaps relating to the impact of external (CP) hydrogen charging on material properties and hard spot cracking of pipelines.
Goal/Deliverables: Report outlining results of laboratory testing that was conducted under conditions considered representative of real-life pipe soil exposure to CP.
Challenges Risks & Mitigations: Creation of laboratory crack failures of hardened tension specimens proved more difficult than anticipated. Project pivoted with increased focus on assessment of hydrogen charge rate, and modifications to enhance crack probability.
Strategic Driver Alignment: Confirm the fundamental integrity and safe operation of vintage pipelines by reducing the uncertainty of fitness for purpose methodologies, including defining critical feature dimensions, associated models and response criteria.
Time Line
Stage one, duration 4-6 months
Revised accelerated testing of notched specimens in hydrogen promoting soil conditions
Stage two, duration 6-14 months
Further development of Phase 2 and 3 work on material property impacts of natural hydrogen charging of susceptible specimens. Refinement of CP impact/potential limits.
Budget = $479,238 – Invoiced to date $133,772.96
Overbudget w.r.t. original work scope
Project plans to modify scope to fit original budget
  Specifically, reduction of evaluation matrix
  Other modifications A/R
Team Leader | Trevor Place, Enbridge | Project Completion Estimation | Q4 2026
TC Chair | Mohsen Achour, ConocoPhillips | TRL at Delivery | 4-5: Operators will be able to make better informed integrity management decisions about HSC at conclusion
Member Beneficiaries | Project was intended to guide CP systems managers. Project data will help pre-empt prescriptive regulation of HSC susceptible pipe with respect to CP operating limits. | Pilot/Field trial needed? If yes, where & target date | No pilot, this is laboratory research
Confirm the fundamental integrity and safe operation of vintage pipelines by expanding the applicability and reducing the uncertainty of Fitness for Service methodologies, including defining critical feature dimensions, associated models & response criteria.
Notes: A one pager is required – it is to be one page so you need to be concise in your message.
Technology Readiness level (TRL) stage needs to be projected out to the end of the current year under review – let the peer reviewers understand what progress you intend to make this year. If possible show movement from to……………….
Pilot/Field trial – this is intended to be who or what member will benefit or trial the technology first – who is in effect your launch customer.
If there are risks explain them and what mitigation you have or may need to address them. Statements that say no risk are acceptable but be prepared to be challenged if there is zero risk especially at low TRL’s where is the R&D?
Goal/Deliverables – explain concisely what the project aims to and will deliver as tangible results – explain in terms of how the industry will use the output from your R&D
Total Investment table – show all years unless project has been very long then show current year, out years and before current year you can show total to date. Note this example has no 2017 as the project should end in 2016. Funding shall be shown in US Dollars (k = thousands).

## Slide 3: TC Research Area Name: CORR – Crack Management (Part of SRP) Idea/Project Name: EC-02-14 Develop Best Practice Guidelines for Application of Machine Learning in Integrity Management Decisions Research Objective Alignment: Define, understand, and improve the key practices, including models, involved with the design, construction, and integrity management of pipelines and related facilities.
Idea/Project Overview
Brief description of technology: The main objective of this project is to develop a guidance document on the application of ML for integrity related decision making. This will include specific use cases, example implementations, and interpretation/visualization of results, of ML methods.
Goal/Deliverables: Guidance document on the application of machine learning with demonstrated case study.
Challenges Risks & Mitigations: Case study requires data from operator members, adds some uncertainty to timelines given differences in internal processes to share data. Sufficient amount of data has been collected to allow the case study.
Strategic Driver Alignment: This project is part of Crack Management SRP. Application of the case study is on SCC susceptibility.
Time Line
Stage one, duration 6-8 months
Drafting the machine learning guidance document
Collect data for the case study
Stage two, duration 16-18 months
Expert peer review of guidance document
Perform the case study
Deliver the final report
Budget: $242,400 – Invoiced to date $107,742
Team Leader | Mohammad Al-Amin, TC Energy | Project Completion Estimation | December 2025
TC Chair | Mohsen Achour, ConocoPhillips | TRL at Delivery | The final outcome of this project is a guidance document for application of machine learning for pipeline integrity management decisions.
Member Beneficiaries | Pipeline Integrity professionals can leverage the final report to develop ML models/methods for solving complex problems by utilizing the vast amount of data collected during pipeline system operation and maintenance activities. | Pilot/Field trial needed? If yes, where & target date | No pilot needed
Notes: A one pager is required – it is to be one page so you need to be concise in your message.
Technology Readiness level (TRL) stage needs to be projected out to the end of the current year under review – let the peer reviewers understand what progress you intend to make this year. If possible show movement from to……………….
Pilot/Field trial – this is intended to be who or what member will benefit or trial the technology first – who is in effect your launch customer.
If there are risks explain them and what mitigation you have or may need to address them. Statements that say no risk are acceptable but be prepared to be challenged if there is zero risk especially at low TRL’s where is the R&D?
Goal/Deliverables – explain concisely what the project aims to and will deliver as tangible results – explain in terms of how the industry will use the output from your R&D
Total Investment table – show all years unless project has been very long then show current year, out years and before current year you can show total to date. Note this example has no 2017 as the project should end in 2016. Funding shall be shown in US Dollars (k = thousands).

## Slide 4: TC Research Area Name: Internal Corrosion Management and Mitigation Idea/Project Name: IC-07-07 Gap analysis for internal corrosion management on deadlegs Research Objective Alignment: Define, understand and improve the key practices, including models, involved in the design, construction and integrity management of pipelines and related facilities.
Idea/Project Overview
Brief description of technology: The project address internal corrosion management in pipeline dead legs (stagnant or low flow piping sections that pose significant corrosion risk). Through a three-phase approach, the research will establish a framework, conduct operator interview and literature review to identify gaps in current practice and develop a strategic roadmap of research projects.
Goal/Deliverables:
A dead leg management framework
Report summarizing the findings from the operator interviews, including a summary of current industry practices, gaps identified and categorized by framework element, barrier and priority and any additional gaps identified
Catalog of literature and technology tagged to the specific parts of the dead leg management framework and identified gaps
A list of identified gaps organized and prioritized with a summary of the current state of each gap including relevant document & technologies.
A written roadmap that details actions, timeline and responsivities
Challenges Risks & Mitigations:
Low Operator participation and Various dead leg configuration & operation condition which shall be addressed through diverse interview and questionnaire approach and one to one discussion with operators
Strategic Driver Alignment:
Define, understand and improve the key practices involved in integrity management of dead legs and create roadmap for future PRCI projects
Time Line
The project starts on June 2025 and end on Feb 2026
The project has five milestones:
  Framework Development & Operator Interview
  Literature Review & Cataloging
  Roadmap Development
  Draft Report
  Final Report
Budget
The budget is allocated for 2025 for a total of $75,000 ($0 invoiced to date)
  Phase 1: Workshop & Interviews - $20,000
  Phase II: Literature & Technology Review - $20,000
  Phase III: Develop Roadmap - $14,000
  Draft & Final Report - $21,000
Team Leader | Abdullah Aldulaijan, Aramco | Project Completion Estimation | Q1 2026 (Shifted from original plan Q4 2025)
TC Chair | Mohsen Achour, ConocoPhillips | TRL at Delivery | 4-5, operators will be able to make better informed decision on dead leg management
Member Beneficiaries | Project is intended to conduct gap analysis and understand operators current practice and challenges associated with dead legs management and provide framework as a guide. This will be used to guide future PRCI research and aid operators in their day to day activates | Pilot/Field trial needed? If yes, where & target date | No pilot or field work trial needed
Notes: A one pager is required – it is to be one page so you need to be concise in your message.
Technology Readiness level (TRL) stage needs to be projected out to the end of the current year under review – let the peer reviewers understand what progress you intend to make this year. If possible show movement from to……………….
Pilot/Field trial – this is intended to be who or what member will benefit or trial the technology first – who is in effect your launch customer.
If there are risks explain them and what mitigation you have or may need to address them. Statements that say no risk are acceptable but be prepared to be challenged if there is zero risk especially at low TRL’s where is the R&D?
Goal/Deliverables – explain concisely what the project aims to and will deliver as tangible results – explain in terms of how the industry will use the output from your R&D
Total Investment table – show all years unless project has been very long then show current year, out years and before current year you can show total to date. Note this example has no 2017 as the project should end in 2016. Funding shall be shown in US Dollars (k = thousands).

## Slide 5: TC Research Area Name: Crack Management Idea/Project Name: SCC-05-04 Cathodic Protection Criteria in Relation to SCC Research Objective Alignment: Define, understand and improve the key practices, including models, involved in the design, construction and integrity management of pipelines and related facilities.
Idea/Project Overview
Brief description: PRCI Project Team identified the need to better understand the operational and environmental conditions that are needed to successfully control corrosion using 100 mV shift criterion with high pH SCC (HpHSCC) susceptible pipe.
Goal/Deliverables: The primary objective of this Phase 1 project is to rigorously assess the 100-mV polarization criterion for controlling HpHSCC in pipelines. Current understanding suggests that the 100mV polarization shift, originally established to mitigate SCC at localized anodic sites, may play a role only during Stage 2 crack growth—if at all. However, Stage 2 represents only a small fraction of a pipeline’s total service life due to its high crack growth rate (~3 mm/yr at 10⁻⁷ mm/s).
Challenges Risks & Mitigations: Collection of soil samples from member Operators.
Strategic Driver Alignment: The report will identify the operational and environmental parameters that affect the likelihood of high pH SCC when the 100mV potential shift criterion is employed to prevent corrosion. These parameters should include soil, temperature, coating type, operating stress, etc.
Time Line
Year One – Baseline data collection, experimental setup, and preliminary modeling.
Year Two – Mechanistic analysis, model refinement, and hybrid CP testing.
Year Three – Field validation, strategy finalization, and industry dissemination.
Budget: $300,000 – Invoiced to date $45,000
Team Leader | Charles Ratts, Williams | Project Completion Estimation | Fall 2028
TC Chair | Mohsen Achour, ConocoPhillips | TRL at Delivery | 3 – Active R&D Proof of Concept
Member Beneficiaries | Pipeline integrity engineers; Corrosion and CP specialists; Operations and maintenance managers; Integrity management software developers; Field personnel involved in mitigation planning and ILI validation. | Pilot/Field trial needed? If yes, where & target date | No pilot needed
Notes: A one pager is required – it is to be one page so you need to be concise in your message.
Technology Readiness level (TRL) stage needs to be projected out to the end of the current year under review – let the peer reviewers understand what progress you intend to make this year. If possible show movement from to……………….
Pilot/Field trial – this is intended to be who or what member will benefit or trial the technology first – who is in effect your launch customer.
If there are risks explain them and what mitigation you have or may need to address them. Statements that say no risk are acceptable but be prepared to be challenged if there is zero risk especially at low TRL’s where is the R&D?
Goal/Deliverables – explain concisely what the project aims to and will deliver as tangible results – explain in terms of how the industry will use the output from your R&D
Total Investment table – show all years unless project has been very long then show current year, out years and before current year you can show total to date. Note this example has no 2017 as the project should end in 2016. Funding shall be shown in US Dollars (k = thousands).

## Slide 6: TC Research Area Name: CORR: Internal Corrosion Management and Mitigation Idea/Project Name: Idea 3712 Testing the effectiveness of different types of maintenance pigs to clean pipelines Research Objective Alignment: Define, understand and improve the key practices involved in integrity management of pipelines and related facilities.
Idea/Project Overview
Brief description of technology: Project aims to address knowledge gaps relating to application-specific cleaning pig selection (e.g., cleaning corrosion pits, removing water, removing biofilms, etc.).
Goal/Deliverables: Report outlining results of flow loop and/or pull-through testing to measure the effectiveness of pigs in various cleaning applications.
  Obtain pipe with features/pits of various sizes. For each cleaning application, “dirty” the pipe as desired (e.g. paraffin, sludge, scale).
  Select pig design parameters to vary (e.g., disc urethane hardness/percent oversize, bypass percent/port orientation, brush orientation/material/thickness/flexibility, magnet strength/placement).
  Measure the volume and depth of material removed per pig pass.
Challenges Risks & Mitigations:
  The experimental design was planned to be informed by IC-07-05, Industry survey on the effectiveness of different types of maintenance pigs to clean pipelines.
  Based on initial results from the survey, there is not clear alignment on which pig design features should be prioritized for testing (wide variation in pigging practices).
  Additional work is needed to better identify gaps for testing—perhaps via workshops.
Strategic Driver Alignment:
  Define, understand and improve the key practices involved in integrity management of pipelines and related facilities.
Time Line
2-year project (TBD based on test scope)
IC-07-05 recommendations:
  Flow loop testing (previous work was pull-through)
  ≥ 10-inch diameter (previous work was 4-inch)
  Evaluate multiple flow velocities to simulate operating conditions
Budget
Guess – Initial estimate: $500,000
Year 1 - $300,000
Year 2 - $200,000
Team Leader | Steven Arnold, Flint Hills Resources | Project Completion Estimation | TBD
TC Chair | Mohsen Achour, ConocoPhillips | TRL at Delivery | 5-6: Operators will be able to make better informed decisions on selection/design of maintenance pigs for the cleaning applications tested
Member Beneficiaries | Maintenance (cleaning) pigging program owners | Pilot/Field trial needed? If yes, where & target date | Pull-through or flow loop testing. Location and date TBD.
Notes: A one pager is required – it is to be one page so you need to be concise in your message.
Technology Readiness level (TRL) stage needs to be projected out to the end of the current year under review – let the peer reviewers understand what progress you intend to make this year. If possible show movement from to……………….
Pilot/Field trial – this is intended to be who or what member will benefit or trial the technology first – who is in effect your launch customer.
If there are risks explain them and what mitigation you have or may need to address them. Statements that say no risk are acceptable but be prepared to be challenged if there is zero risk especially at low TRL’s where is the R&D?
Goal/Deliverables – explain concisely what the project aims to and will deliver as tangible results – explain in terms of how the industry will use the output from your R&D
Total Investment table – show all years unless project has been very long then show current year, out years and before current year you can show total to date. Note this example has no 2017 as the project should end in 2016. Funding shall be shown in US Dollars (k = thousands).