## Slide 1: Current Project and New Idea Review
2026-10-22
Integrity & Inspection Technical Committee
Committee Chair: Paul Monsour, SoCalGas
PRCI Support Staff: Jim Wayman

## Slide 2: Integrity & Inspection Project Review
MAT-7-2B: Improving NDE efficiency, detection, and characterization of hard spots
  The proposed research will target accuracy improvements and efficiency of in-ditch evaluation methods of hard spots. The project will seek to improve methods to more accurately and more efficiently characterize in-ditch hard spots as well as reduce conservatism for evaluating hard spot anomalies identified from ILI results.
NDE-3-7: Verification of Current Magnetometry Inspection (CMI) Technology for Non-Intrusive External Corrosion Detection & Assessment
  The research will evaluate the use of Current Magnetometry Inspection (CMI) – which uses active magnetometry approach - for remote, precise, non-contact evaluation of external corrosion for non-piggable (or difficult-to-inspect) pipelines.

## Slide 3: Integrity & Inspection Project Review
SCC-06-06: Defining threshold below which SCC is not detrimental to pipeline integrity in normal operation
  The research will produce a threshold under which SCC will not be considered an active threat. This will allow operators to focus resources on appropriate pipeline risks and improve system integrity.
Idea 3792: Selective Seam Weld Corrosion (SSWC) Susceptibility Tests
  Developing a test method for classifying pipe into populations that are and are not susceptible to SSWC would be beneficial to pipeline operators in the integrity management of the SSWC threat. Currently, PHMSA requires operators to treat all ERW and flash welded pipe as susceptible to SSWC.

## Slide 4: Improving NDE efficiency during Hard Spot Assessment
Pipeline Integrity Engineer, TC Energy
Nashville, TN
Oct 23, 2025
Patrick Adamski
Project # MAT-7-2B
Notes: Template last revised 01/25/25, AMV
Notes:
The research contractor can add their company logo onto the left side of this cover slide.
Anything between the square brackets ([]) inclusive should be replaced.
There are two sections in this presentation, one for project status updates, the other for project final results. Delete the section that isn’t applicable.
This template is for project status updates or for the presentation for project final results presented at PRCI technical committee (TC) meetings. It may also be used for project team updates as an option.
  Project updates presented at PRCI technical committee meetings should focus on changes in project status since the last TC update was presented.
    Limit the background information that is presented at every TC meeting. More background information may be necessary if an update was not provided at the previous TC meeting. Work with the PRCI Program Manager (PM) and project team leader to verify the appropriate level of background information.
    PRCI posts presentations given at previous TC meetings, assume that the audience has already seen most of that information.
    As a general rule, status updates should be 20-30 minutes in length. Coordinate the presentation time with the PRCI PM.
    Unless directed otherwise by the PM, status updates should not be a working session for the project team. Any new issues raised in this review should be taken offline to be addressed at a project team meeting or via PRIME/email.
  Project final results
    Project final results should include high level background information
    As a general rule, project final results should be 30-60 minutes in length. Coordinate the presentation time with the PRCI PM.

## Slide 5: MAT-7-2B - Overview
Principal investigator: RSI /SI
PRCI Project Team Leader: Patrick Adamski
Total costs: $200,000
Background:
Project intends to target accuracy improvements and efficiency of in-ditch evaluation methods of hard spots. The project will seek to improve methods to more accurately and more efficiently characterize in-ditch hard spots as well as reduce conservatism for evaluating hard spot anomalies identified from ILI results.
Research Objectives/Project Deliverables:
Test screening methodologies (ECA, polishing/etching)
Test Characterization methodologies (ECA, portable hardness testing)
Other technologies identified (UT Rayleigh waves, pulsed ECA, electrical resistivity tomography)

## Slide 6: Verification of Current Magnetometry Inspection (CMI) Technology for Non-Intrusive External Corrosion Detection & Assessment
Research Idea in PRIME: PRCI PRIME 2.0
Engineer III – Acuren, Inc.
Magnolia, TX
October 10, 2025
Parth Patel
Project # NDE-03-07

## Slide 7: NDE-3-07: Project Overview
Principal investigator: Parth Patel
PRCI Project Team Leader: David Xu, PGE
Background: The project aims to improve understanding of Current Magnetometry Inspection (CMI) technology to detect external corrosion
Research Objectives/Project Deliverables: The project will bury a set of pipes at PRCI TDC facility with known features and coordinate inspection with EMPIT and EMPACT AI
NDE-3-07 CMI Technology Verification

## Slide 8: Goals for Project
Determine CMI accuracy for detecting and locating corrosion
Determine if CMI can classify between passive and active corrosion
Identify limitations for coating defects and coating types
Explore CMI abilities concerning coating disbondment
Determine Empact AI capabilities and utilization
Validation of CMI for real-world use cases
Explore effects of pressure on the technology response
Provide framework for incorporating CMI into traditional ECDA processes
Literature Survey – Equip operators with digestible summary of current state of the art magnetometry technologies

## Slide 9: Defining Threshold Below Which SCC Is Not Detrimental to Pipeline Integrity in Normal Operation
Sr Engineer, DNV
Nashville, TN
October 22, 2025
Ben Hanna, PhD
Project # SCC-06-06
Project Status Update

## Slide 10: SCC-06-06: SCC Threshold
DNV going through internal database to classify/quantify SCC growth
Beginning to summarize industry practices from available reports/papers
Project on budget and on schedule
Way of estimating SCC growth rate
DNV to continue to go through databases to collect data
Have draft language for literature review
14-month schedule (August 2025– October 2026)
MS 01-01 – Literature Review
MS 01-02 – Document Current Industry Practices
$8,127 of $54,700 USD (15% of 2025 budget)
Have not received any data from member companies. Did request form go out?
Overall schedule on track at this time
Received 2025 PO for $54,700

## Slide 11: MS-01-01 Literature Review
Compile info on failures, near misses, inspection results, FFS analyses, failure analyses.
  Been using internal database, but need info from member companies
Relate SCC type (near-neutral pH, high-pH), extent (size), burst pressure, growth rates, calculated remaining lives to operating conditions (%SMYS).
Using “Installation + 10 yrs” as SCC initiation rule of thumb.
MS 01-01

## Slide 12: Desktop or Laboratory (optional) Study
Use results from Phase I to correlate SCC growth rates to stress level and pressure cycle history using metallurgical measurements and industry models (e.g., Beavers’ model).
Monte Carlo simulations to predict probability of failure at various stress levels, pipe properties, and cyclic loading.
  Leverage with existing risk models to inform integrity decisions
OPTIONAL: Hole drilling method on lower stress pipe (< 30%SMYS) to investigate whether residual stresses are present.
  10 tests – 7 on pipe with SCC, 3 on pipe without
Deliverable – Incorporated into a draft report for project team feedback.
MS 02-01

## Slide 13: Phase 1 - Standardized SSWC Susceptibility Testing & Phase 2 – SSWC/LOF Interaction
Research Idea in PRIME: PRCI PRIME 2.0
Energy Transfer
Nashville I&I Meeting
October 23, 2025
Lee Sellers
Idea #3792
Notes: Template last revised 01/25/25, AMV
Notes:
The research contractor can add their company logo onto the left side of this cover slide.
Anything between the square brackets ([]) inclusive should be replaced.
There are two sections in this presentation, one for project status updates, the other for project final results. Delete the section that isn’t applicable.
This template is for project status updates or for the presentation for project final results presented at PRCI technical committee (TC) meetings. It may also be used for project team updates as an option.
  Project updates presented at PRCI technical committee meetings should focus on changes in project status since the last TC update was presented.
    Limit the background information that is presented at every TC meeting. More background information may be necessary if an update was not provided at the previous TC meeting. Work with the PRCI Program Manager (PM) and project team leader to verify the appropriate level of background information.
    PRCI posts presentations given at previous TC meetings, assume that the audience has already seen most of that information.
    As a general rule, status updates should be 20-30 minutes in length. Coordinate the presentation time with the PRCI PM.
    Unless directed otherwise by the PM, status updates should not be a working session for the project team. Any new issues raised in this review should be taken offline to be addressed at a project team meeting or via PRIME/email.
  Project final results
    Project final results should include high level background information
    As a general rule, project final results should be 30-60 minutes in length. Coordinate the presentation time with the PRCI PM.

## Slide 14: Objective #1 – Standardized SSWC Lab Test
Two test methods were studied in EC-2-12:
  Accelerated Dissolution Test (AD), and
  Linear Polarization Resistance (LPR) Test
DNV has applied a ‘standard’ version of the AD test to evaluate the SSWC susceptibility of autogenous seam welds
Results have been encouraging
  Modern pipe, believed to be non-susceptible, produced no or very shallow grooves
  Pipe removed from service with SSWC flaws produced grooving ratios up to 3
The objectives of this project are to
  Refine and further develop the ‘standard’ test method, and
  Benchmark the test results against real-world SSWC pipe samples to bound what the growth rate may be at the seam.
Notes: Can be more than one slide. Assume the audience has seen the last presentation provided in this venue (e.g., if presented at a project team meeting, the project team has seen the previous set of slides presented to the project team; if presented at a TC meeting, the TC has seen the slides presented at the last TC meeting
Only use if more detail is needed than presented on the overview slide

## Slide 15: Objective #2 – Benchmarking SSWC Growth Rates
Susceptibility Benchmarking
  Define test results (grooving ratios) that can be used to classify pipe as susceptible or non-susceptible.
  Analyze results to benchmark AD test results against SSWC susceptibility and severity rating.
  Procure and test samples of susceptible and non-susceptible pipe types:
    Susceptible - exhibited SSWC flaws in the field or experienced leaks/ruptures
    Non-susceptible - corrosion across the seam with absence of preferential attack
SSWC Growth Rate Benchmarking
  Compare growth at and away from the (susceptible) seam to bound what the growth rates may be.
  Is grooving ratio relevant to the SSWC growth rate?
  Does SSWC grow any faster than a corrosion cell adjacent to the seam?
  What conditions effect the SSWC growth rate?
Notes: Use industry pipe to get distribution of depths/growth rates. Then relate that to bench scale tests.
Other operators likely to use test to validate susceptibility

## Slide 16: Phase 2 - Objective #1 – SSWC/LOF Interaction
SSWC may intersect manufacturing flaws on/near the bond line. The shape and further corrosion behavior of the resulting combined flaw are unknown.
Surface-breaking manufacturing flaws are typically covered with a dark-colored, high-temperature oxide layer. If the oxide layer is more resistant to further SSWC than other weld metal, the flaw shape may remain relatively narrow along the LOF, compared to other SSWC flaws.
We’ve seen cross-sections of these flaws that suggest narrow LOF defects being corroded along its walls faster than at the tip to form the classic v-shape.
Energy Transfer has obtained samples of an ERW seam with known LOF defects that appear to have formed SSWC.
  What shape is produced when SSWC intersects a pre-existing LOF?, and
  Does the combined defect continue to grow by SSWC and at the same rate as before the intersection?
Notes: Can be more than one slide. Assume the audience has seen the last presentation provided in this venue (e.g., if presented at a project team meeting, the project team has seen the previous set of slides presented to the project team; if presented at a TC meeting, the TC has seen the slides presented at the last TC meeting
Only use if more detail is needed than presented on the overview slide

## Slide 17: Objective: Effects of Pre-existing Flaws
Nature of Growth from Pre-existing Flaws
  Qualitatively show the morphology of corrosion attack of pre-existing flaws and whether it creates a classic v-shape that might be misconstrued as a grooving ratio.
A testing matrix will be developed to perform triplicate tests on:
  Investigate the effect of SSWC interacting with bond line defects, such as LOF, including combined flaw shape and further SSWC growth rate.
    Remove samples from solution at various intervals to capture stages of growth.
Quantify the growth at the seam
  The samples removed at different time intervals will be compared with bounded values estimated from Phase I of Idea #3792.
  This will provide guidance on what growth rates to use in FFS analyses.
Notes: Can be more than one slide. Assume the audience has seen the last presentation provided in this venue (e.g., if presented at a project team meeting, the project team has seen the previous set of slides presented to the project team; if presented at a TC meeting, the TC has seen the slides presented at the last TC meeting
Only use if more detail is needed than presented on the overview slide